## Slide 1: MIM/MOSCAP Electrical Characterizations
Akash Levy, Jung-Soo Ko

## Slide 2: Characterized Structures
N-type highly phosphorus-doped very low resistivity (0.01-0.09 Ω cm) wafers
  This should be close to a MIM structure
  10nm (100 cycles) thermal ALD alumina
  No seed layer
Rest are stockroom I-test wafers: P-type boron-doped w/resistivity 0.1-0.9 Ω cm
AJA-deposited Al seed layer (nm) | Fiji2-deposited thermal alumina (nm)
0.5 | 5 (first)
1 | 5
1.5 | 5
0.5 | 10 (second)
1 | 10
1.5 | 10
2 | 10
2 | 10

## Slide 3: Back-gate contact
Scratch surface for probe
Breakdown MIM structure
Use broken-down MIM structure as back-gate contact
Advantage: physically closer to structures being tested so less IR drop

## Slide 4: Breakdown I-V Curves

## Slide 5: Breakdown I-V Curves

## Slide 6: Breakdown I-V Curves

## Slide 7: Breakdown I-V Curves

## Slide 8: Breakdown I-V Curves

## Slide 9: Breakdown I-V Curves

## Slide 10: Breakdown I-V Curves

## Slide 11: Breakdown I-V Curves

## Slide 12: MIM: 10 nm ALD alumina (no seed)
Chart: Representative C-V plot
Capacitance is roughly constant
No depletion/inversion effects seen really
This is probably because the Si substrate is highly-doped and thus behaves almost metallically
Parallel plate capacitor approximation
Area of MIM structure:
Woollam measured thickness: 10.9 nm
Expected k: 7.8 – 11.1
Fitted k: 6
Fitted oxide thickness with k=7.8: 14.18 nm

## Slide 13: C-V Curves

## Slide 14: C-V Curves

## Slide 15: C-V Curves

## Slide 16: C-V Curves with Possible Soft Breakdown

## Slide 17: C-V Curves with Possible Soft Breakdown

## Slide 18: TODOs on data analysis
Will fit C-V curves to determine doping density and oxide capacitance
Will plot breakdown voltage as a function of seed/oxide thickness
Will try to fit breakdown behavior in soft breakdown regime