## Slide 1: Plans when AJA training is done!
Akash, Jungsoo

## Slide 2: Effect of Seed Layer
Control: w/ and w/o seed layer on Si (No 2D)
Control sample: thickness(=t)
W/O seed layer process:
  Si waferclean(Do you think this is necessary? Right after we get it from storage room into cleanroom), wet bench cleanALD(Fiji2)measure t (Woollam)metal deposition for top electrode(Lesker/AJA)-CV measurement (micromanipulator)
W/ seed layer process:
  Si wafercleanSeed layer(AJA)expose in airmeasure t (Woollam)ALDmeasure t (Woollam)metal deposition(Lesker/AJA)CV measurement (micromanipulator)
These are with Silicon substrate, so this can be carried out parallel with bunch of varied parameters
This comparison will show the effect from seed layer on film quality
How to figure out whether the seed layer at the interface with substrate is conductive or not?

## Slide 3: Seed Layer in MoS2
W/O Seed layer:
  MoS2 samplesAFM/SEMALD(Fiji)WoollamAFM/SEM(if CV measurement seems to work with very thin semiconductor layermetal deposition(AJA)CV measurement)
    Try 5nm 10nm ALD to see that it doesn’t grow well without seed layer
W/ Seed layer:
  MoS2 samplesAFM/SEMAJA seedlayerAFM/SEMWoollamALDWoollamAFM/SEM(if CV measurement seems to workmetal deposition(AJA)CV measurement)
    Oxidized seed layer will be thicker than deposited thickness since it is oxidized and is expected to make is very discernable through AFM and SEM
We can verify from experiment 1 without seed layer that ALD does not really work for 2D films, so from experiment 2, we can verify that we need seed layer for conformal coverage
If electrical measurement seems difficult with MoS2, investigate more on full coverage this quarter and try to investigate on methods for electrical measurements afterwards
  But still, effect of seed layer on electrical performance can be verified through previous experiments

## Slide 4: Things to do with MoS2 samples
AFM on SiO2 only areas and see the roughness there
AFM on SiO2 substrate before anything is grown
SEM on MoS2 samples
If we can discern what is MoS2 and what is oxidized seed layer (or ALD grown oxide) on the surface of each MoS2 flakes, does the roughness of each flake matter?

## Slide 5: Check list
Initial plan is to see the full coverage on MoS2 differentiating seed layer thicknesses
  Find the thinnest seed layer we can go that guarantees conformal coverage
After seed layer deposition, they oxidize and how deep the oxidation goes through should be checked!
  Find methods on how to verify if it has been fully oxidized or if there still exist part where it is conductive
Need four MoS2 samples for Al deposition run for different 4 thicknesses seed layer
Need four samples more when Hf source is available for different 4 thicknesses
Need to make carrier wafer  not necessary
If highly-doped Si is to be used, it should be sawed  ask someone trained on DISCO  Check!
If Si wafer (4inch) is used, then is the cleaning really necessary after we get it from storage room?
With Woollam, can we do the measurement of large area?  yes, but check how to do this!
If total 10nm is target thickness, can we do 5nm ALD first and do all the measurements, then 5nm ALD afterwards and do measurements to save the number of MoS2 samples?

## Slide 6: Tables to fill in (for seed layer effect)
Seed layer (Al) | Thickness(Woollam) | Rougness(AFM) | Coverage(SEM) | Capacitance | Leakage
0.5nm (Al) |  |  |  |  | 
1nm (Al) |  |  |  |  | 
1.5nm (Al) |  |  |  |  | 
2nm (Al) |  |  |  |  | 
Seed layer (Hf) | Thickness(Woollam) | Rougness(AFM) | Coverage(SEM) | Capacitance | Leakage
0.5nm (Hf) |  |  |  |  | 
1nm (Hf) |  |  |  |  | 
1.5nm (Hf) |  |  |  |  | 
2nm (Hf) |  |  |  |  | 
 | Before ALD |  |  |  |  | After ALD (Total 5nm) – after 10nm is done |  |  |  |  | After ALD (Total 10nm) |  |  |  | 
Seed layer | Thickness(Woollam) | Rougness(AFM) | Coverage(SEM) | Capacitance | Leakage | Thickness(Woollam) | Rougness(AFM) | Coverage(SEM) | Capacitance | Leakage | Thickness(Woollam) | Rougness(AFM) | Coverage(SEM) | Capacitance | Leakage
No seed layer |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
0.5nm (Al) |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
0.5nm (Hf) |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
1nm (Al) |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
1nm (Hf) |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
1.5nm (Al) |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
1.5nm (Hf) |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
2nm (Al) |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
2nm (Hf) |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 7: MoS2 samples (electrical measurement is expected to be taken but possibly towards the end of this quarter)
Seed layer (Al) | Thickness(Woollam) | Rougness(AFM) | Coverage(SEM) | Capacitance | Leakage
0.5nm (Al) |  |  |  |  | 
1nm (Al) |  |  |  |  | 
1.5nm (Al) |  |  |  |  | 
2nm (Al) |  |  |  |  | 
Seed layer (Hf) | Thickness(Woollam) | Rougness(AFM) | Coverage(SEM) | Capacitance | Leakage
0.5nm (Hf) |  |  |  |  | 
1nm (Hf) |  |  |  |  | 
1.5nm (Hf) |  |  |  |  | 
2nm (Hf) |  |  |  |  | 
 | Before ALD |  |  |  |  | After ALD (Total 5nm) – after 10nm is done |  |  |  |  | After ALD (Total 10nm) |  |  |  | 
Seed layer | Thickness(Woollam) | Rougness(AFM) | Coverage(SEM) | Capacitance | Leakage | Thickness(Woollam) | Rougness(AFM) | Coverage(SEM) | Capacitance | Leakage | Thickness(Woollam) | Rougness(AFM) | Coverage(SEM) | Capacitance | Leakage
No seed layer |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
0.5nm (Al) |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
0.5nm (Hf) |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
1nm (Al) |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
1nm (Hf) |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
1.5nm (Al) |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
1.5nm (Hf) |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
2nm (Al) |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
2nm (Hf) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |