## Slide 1
ENGR 241: ALD Process for Top-Gating 2D Materials
Akash Levy, Jung-Soo Ko
Mentors: J Provine, Michelle Rincon, Vijay Narasimhan
Stanford Nanofabrication Facility, Stanford University, Stanford, CA
AFM HERE
Introduction
2D materials  high mobility and little SCE when scaled (no dangling bonds at the surface)
2D TMDs Scalability, low off-state energy consumption, flexibility, large bandgap
Challenges & Proposal
High-k needs to be stacked for CMOS compatibility
 Use atomic layer deposition (ALD)
ALD on 2D materials is difficult due to lack of dangling bonds
Surface treatment is necessary for low EOT devices
Surface Characterization
Seed layer deposition (0.5, 1, 1.5, 2nm) on MoS2 and ALD total of 5 and 10nm of alumina
  Ellipsometry for seed layer thickness & AFM for roughness
  Define # of ALD cycles based on oxidized alumina thickness
Electrical Characterization
Conclusion
Seed layer deposition helps nucleation for ALD
  Thicker seed layer smoothens the surface  conformal coverage
Seed layer seems to increase dielectric constant and decrease breakdown voltage (based on MIM structures)
Need more data to fully verify: will also test with hafnia
Mark location on chip first to measure on same flake
  More accurate but possible PR residues
(a)
(b)
(a) Bandgap (b) mobility trend of 2D TMDs [1, 2]
(a)
(b)
100nm
(a) Non-uniform ALD on 2D materials [3], (b) AFM after ALD w/o seed layer (5nm left, 10nm right) on MoS2 , (c) Proposed seed layer deposition process
References
[1] Duan et al. Chem. Soc. Rev., 2015, 44, 8859
[2] C. English, PhD Thesis, Stanford, Dec 2017
[3] Park et al. RSC Adv., 2017, 7, 884
(c)
Next Quarter Plan/Process
FET device process flow for I-V measurement
    C-V difficult due to ultrathin channel
Different seed layer and ALD oxide combinations
    Al, Hf, Zr
    Various available oxides in Fiji
PEALD on 2D materials w/, w/o seed layer
    Plasma may damage 2D materials
    Seed layer deposition may protect from plasma damage
Proposal: Seed Layer Deposition prior to top gating
    Seed layer on 2D TMDs helps nucleation for ALD growth
SiO2
2D TMD
Evaporated Seed Layer
Gate Oxide
Si
SiO2
Oxidized Seed layer
Metal Oxide
Si
SiO2
Seed layer
Si
SiO2
AJA
Si
SiO2
Oxidized seed layer
Air
Fiji
Chart: Alumina w/ Seed Layer
| 0.5 | 1 | 1.5 | 2
Total 5nm | 537 | 505 | 400 | 245
Total 10nm | 428 | 307 | 276 | 204
Chart: Alumina Thickness
| 0.5 | 1 | 1.5 | 2
After Oxidized | 1.0095 | 1.772 | 2.6545 | 3.8065
S
D
Si
SiO2
HKMG
G
MoS2 Sample
Contact Pads (Litho & AJA)
HKMG Seed layer (AJA)
ALD(Fiji 1/2)
Gate Electrode (AJA)
Liftoff
Litho (S/D patterning)
S/D Electrode (AJA)
Liftoff
Litho (Gate Patterning)
Litho (Channel Patterning)
O2 Plasma etch
Benefit to SNF
Process flow for top-gated 2D devices
Recipe for ALD on 2D materials and samples w/ seed layer
Provide characterization results (electrical and surface imaging) regarding
  Different seed layer thickness
  Different seed layer material
(a)
(b)
(a) 2D FET device structure (b) 2D FET device process flow
Chart: MIM: Breakdown Voltage
| 0.5 | 1 | 1.5 | 2
5 nm ALD Layer | 15.8969 | 31.7795 | 21.2339 | 15.2224
10 nm ALD Layer | 40.7277 | 24.6895 | 13.7818
Chart: MIM: Dielectric Constant
| 0.5 | 1 | 1.5 | 2
5 nm ALD Layer | 4.4032 | 4.6983 | 5.1542 | 7.5706
10 nm ALD Layer | 5.9461 | 5.3029 | 5.8046 | 1.7346 | 7.3009
Chart: MIM: Breakdown V vs. ALD Thickness
| 4.2769999999999992 | 4.1429999999999989 | 3.9949999999999997 | 4.6330000000000009 | 10.917999999999999 | 9.4059999999999988 | 9.2949999999999999 | 9.7309999999999999 | 9.6180000000000003
 | 4.9378 | 5.4477 | 4.4085 | 5.7626 | 8.3615 | 9.008 | 9.688 | 9.2078 | 8.8866
Chart: MIM: Measured vs. Target Seed Layer Thickness
| 0 | 0.5 | 1 | 1.5 | 2
 | 0 | 1.227 | 2.361 | 3.475 | 4.327
Type
MIM Structure Doping: highly n-doped (phosphorus) Resistivity: very low (0.01-0.09 Ω cm)
MOS Structure Stockroom I-test wafer Doping: p-doped (boron) Resistivity: moderately low (0.1-0.9 Ω cm)
Seed layer (nm)
0.0
0.5
1.0
1.5
2.0
ALD (nm)
5
10
Chart: Before ALD w/ Seed Layer
| 0nm | 0.5nm | 1nm | 1.5nm | 2nm
 | 0.2 | 0.18333 | 0.705 | 0.48 | 0.679
 | 5nm alumina (oxidized seed layer+ALD) |  |  | 
Seed layer (nm) | 0.5 | 1 | 1.5 | 2
RMS (nm) | 0.538 | 0.505 | 0.400 | 0.245
 | 10nm alumina (oxidized seed layer+ALD) |  |  | 
Seed layer (nm) | 0.5 | 1 | 1.5 | 2
RMS (nm) | 0.428 | 0.307 | 0.277 | 0.205
n++ Si
Native Oxide SiO2 (1.5nm)
AlOx (Evaporated)
Al2O3 (ALD)