## Slide 1: MIM/MOSCAP Electrical Characterizations
Akash Levy, Jung-Soo Ko

## Slide 2: Characterized Structures
N-type highly phosphorus-doped very low resistivity (0.01-0.09 Ω cm) wafers
  This should be close to a MIM structure
  10nm (100 cycles) thermal ALD alumina
  No seed layer
Rest are stockroom I-test wafers: P-type boron-doped w/resistivity 0.1-0.9 Ω cm
AJA-deposited Al seed layer (nm) | Fiji2-deposited thermal alumina (nm)
0.5 | 0 or 1 (???)
1 | 5
1.5 | 5
1 | 10
1.5 | 10
2 | 10
2n (???) | 10

## Slide 3: Back-gate contact
Scratch surface for probe
Breakdown MIM structure
Use broken-down MIM structure as back-gate contact
Advantage: physically closer to structures being tested so less IR drop

## Slide 4: MIM: 10 nm ALD alumina (no seed)
Chart: Dielectric Breakdown
5 samples
100 mA compliance current
Chart: Dielectric Breakdown

## Slide 5: MIM: 10 nm ALD alumina (no seed)
Chart: Representative C-V plot
Capacitance is roughly constant
No depletion/inversion effects seen really
This is probably because the Si substrate is highly-doped and thus behaves almost metallically

## Slide 6: MOSCAP: 0.5 nm seed layer with 1 nm Al2O3
Can see accumulation, inversion, depletion regions
Can see difference between low-freq. and high-freq. C-V curves
Will do fitting to extract parameters soon
Chart: Representative C-V plot

## Slide 7: Rest of the plots to come soon! 
TODO:
  Fit breakdown curves to determine breakdown voltages/behavior
    Don Gardner provided reference for this
    Kolodzey, James, Enam Ahmed Chowdhury, Thomas N. Adam, Guohua Qui, I. Rau, Johnson Olufemi Olowolafe, John S. Suehle, and Yuan Chen. "Electrical conduction and dielectric breakdown in aluminum oxide insulators on silicon." IEEE Transactions on Electron Devices 47, no. 1 (2000): 121-128.
  Make sure MIM’s constant capacitance somewhat matches expected value
    What is ? Need to determine from shadow mask… does Vijay know?
  Fit C-V curves to check parameters like substrate doping and capacitances
  Plot the rest of the data! (Need to write a script to do this)